| ILLUSTRATED REPORT FOR BRILLIANT |  |  | Parameter | Avg | Min | Max | Dev | Cut | Sym |  |  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  | Diameter, mm | 5.851 | 5.838 | 5.865 | 0.46% | E | EX |  |  | 5.852 | 5.844 | 5.847 | 5.851 |  |  |  |  |
|  |  |  |  | Crown angle, ° | 34.50 | 34.13 | 34.74 | 0.61 | Grading | VG |  |  | 34.74 | 34.70 | 34.61 | 34.65 | 34.24 | 34.13 | 34.25 | 34.67 |
|  |  |  |  | Pavilion angle, ° | 41.71 | 41.39 | 42.13 | 0.74 | Grading | VG |  |  | 41.40 | 41.39 | 41.52 | 41.78 | 41.97 | 42.13 | 41.97 | 41.52 |
| Model | st1 |  |  | Total height, % | 61.98 |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |
| Expert name | Makoed A.G. |  |  | Crown height, % | 14.96 | 14.67 | 15.23 | 0.56 | E | EX |  |  | 14.82 | 15.00 | 15.21 | 15.23 | 14.99 | 14.93 | 14.67 | 14.87 |
| Report date | 10.12.2007 |  |  | Pavilion depth, % | 44.40 | 44.05 | 44.73 | 0.68 | N/A | EX |  |  | 44.68 | 44.27 | 44.06 | 44.05 | 44.19 | 44.62 | 44.73 | 44.61 |
| Real weight, ct |  |  |  | Table, % | 56.32 | 56.09 | 56.48 | 0.40 | Grading | EX |  |  | 56.48 | 56.09 | 56.30 | 56.42 |  |  |  |  |
| Calculated weight, ct | 0.74, 0.7451 |  |  | Culet, % | 0.33 | 0.21 | 0.40 | 0.19 | E | EX |  |  |  |  |  |  |  |  |  |  |
| Measurements | 5.851 (5.838-5.865) x 3.626 /0.004 mm |  |  | Girdle Bezel, % | 2.61 | 2.42 | 2.78 | 0.36 | E | EX |  |  | 2.48 | 2.72 | 2.71 | 2.71 | 2.78 | 2.42 | 2.58 | 2.49 |
| Spread | 0.00 ct, 0.24% |  |  | Girdle Bone, % | 2.98 | 2.70 | 3.14 | 0.43 |  | EX |  |  | 2.93 | 2.81 | 3.08 | 3.12 | 2.70 | 3.14 | 2.90 | 3.13 |
| AGS Spread | -0.00 ct, -0.07% |  |  | Girdle Valley, % | 1.17 | 0.96 | 1.39 | 0.43 | E | EX |  |  | 1.29 | 1.23 | 1.14 | 1.21 | 1.10 | 1.17 | 1.22 | 1.11 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | 1.22 | 0.96 | 0.96 | 1.25 | 1.39 | 1.04 | 1.26 | 1.22 |
| Average values, mm |  |  | Star: | 56.02: | 54.07: | 57.10: | 3.03 | E | VG |  |  | 56.64: | 56.75: | 54.07: | 54.49: | 55.70: | 56.92: | 56.49: | 57.10: |
|  |  |  | Upper ratio, % | 43.98 | 45.93 | 42.90 |  |  |  |  |  | 43.36 | 43.25 | 45.93 | 45.51 | 44.30 | 43.08 | 43.51 | 42.90 |
| Diam | Total height | Crown height | Pav. depth | Table | Culet | Girdle |  |  | Star angle, ° | 22.93 | 22.76 | 23.04 | 0.28 |  | EX |  |  | 23.04 | 22.93 | 23.04 | 22.76 | 22.87 | 22.87 | 22.99 | 22.96 |
|  |  |  |  |  |  | Bezel | Bone | Valley |  |  | Upper girdle angle, ° | 41.11 | 40.18 | 42.14 | 1.95 |  | VG |  |  | 41.49 | 41.64 | 42.14 | 41.77 | 41.10 | 40.92 | 41.20 | 40.84 |
| 5.851 | 3.626 | 0.876 | 2.598 | 3.295 | 0.019 | 0.153 | 0.174 | 0.069 |  |  |  |  |  |  |  |  |  |  |  | 41.21 | 40.94 | 40.18 | 40.87 | 40.68 | 40.82 | 40.88 | 41.14 |
|  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % | 80.27 | 78.66 | 81.28 | 2.62 | E | EX |  |  | 78.66 | 79.71 | 79.38 | 78.98 | 80.01 | 80.41 | 79.66 | 81.03 |
|  |  |  |  |  |  |  |  |  |  |  |  | 81.14 | 80.73 | 81.28 | 81.17 | 80.96 | 80.62 | 80.61 | 80.02 |
|  |  |  | Lower girdle angle / Halves angle, ° | 42.72 | 42.22 | 43.27 | 1.05 |  | VG |  |  | 42.22 | 42.33 | 42.37 | 42.53 | 42.46 | 42.70 | 42.94 | 43.04 |
|  |  |  |  |  |  |  |  |  |  |  |  | 43.19 | 43.27 | 43.09 | 43.05 | 42.82 | 42.71 | 42.42 | 42.35 |
|  |  |  | Twist, ° | 0.84 | 0.27 | 1.31 | 1.04 |  | VG |  |  | 0.98 | 1.21 | 0.62 | 1.31 | 1.03 | 0.27 | 0.97 | 0.34 |
|  |  |  | Crown height, mm | 0.876 | 0.858 | 0.891 | 0.033 | E | EX |  |  | 0.867 | 0.877 | 0.890 | 0.891 | 0.877 | 0.874 | 0.858 | 0.870 |
|  |  |  | Pavilion depth, mm | 2.598 | 2.577 | 2.617 | 0.040 | N/A | EX |  |  | 2.614 | 2.590 | 2.578 | 2.577 | 2.586 | 2.611 | 2.617 | 2.610 |
|  |  |  | Table, mm | 3.295 | 3.282 | 3.305 | 0.023 | Grading | EX |  |  | 3.305 | 3.282 | 3.294 | 3.301 |  |  |  |  |
|  |  |  | Culet, mm | 0.019 | 0.012 | 0.023 | 0.011 | E | EX |  |  |  |  |  |  |  |  |  |  |
|  |  |  | Girdle Bezel, mm | 0.153 | 0.142 | 0.163 | 0.021 | E | EX |  |  | 0.145 | 0.159 | 0.159 | 0.158 | 0.163 | 0.142 | 0.151 | 0.146 |
|  |  |  | Girdle Bone, mm | 0.174 | 0.158 | 0.184 | 0.025 |  | EX |  |  | 0.171 | 0.165 | 0.180 | 0.182 | 0.158 | 0.184 | 0.170 | 0.183 |
|  |  |  | Girdle Valley, mm | 0.069 | 0.056 | 0.081 | 0.025 | E | EX |  |  | 0.075 | 0.072 | 0.067 | 0.071 | 0.064 | 0.069 | 0.072 | 0.065 |
|  |  |  |  |  |  |  |  |  |  |  |  | 0.071 | 0.056 | 0.056 | 0.073 | 0.081 | 0.061 | 0.074 | 0.071 |
|  |  |  | Measurement as per OctoNus theory: |  |  |  |
|  |  |  | Crown angle, ° | 34.50 | 34.42 | 34.66 | 0.24 |  |  |  |  | 34.49 | 34.42 | 34.43 | 34.66 |  |  |  |  |
|  |  |  | Pavilion angle, ° | 41.71 | 41.65 | 41.76 | 0.11 |  |  |  |  | 41.68 | 41.76 | 41.74 | 41.65 |  |  |  |  |
|  |  |  | Fish eye effect, ° | 12.35 | N/A |  |  |  | Extra Facet / Nat | No |
|  |  |  | Culet through Crown Bezel, ° | 9.45 | N/A |  |  |  | Girdle to MIC, mm | 0.004 |
|  |  |  | Parameter, ° | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |  |  | Paint / Dug | Avg | Type | Sym | Dev | Sym |
|  |  |  | Pav. azimuths dev. from ideal | 0.00 | -2.43 | -0.06 | -0.28 | -0.31 | -1.19 | 0.06 | -0.14 |  |  | Crown, ° | -1.13 | Painting | EX | -2.21 | EX |
|  |  |  | Crown azimuths dev. from ideal | -0.98 | -1.22 | -0.69 | -1.59 | -1.34 | -0.92 | -0.92 | -0.48 |  |  | Crown, notch. | 0.3, Small |  |  | 0.6 |  |
|  |  |  | Crown painting | -0.77 | -1.36 | -0.11 | -0.80 | -0.84 | -1.35 | -0.30 | -1.16 |  |  | Pavilion, ° | -0.51 | Painting | EX | -2.81 | EX |
|  |  |  |  | 0.02 | -0.75 | -2.16 | -1.57 | -1.37 | -1.65 | -2.21 | -1.67 |  |  | Pavilion, notch. | 0.1, Very small |  |  | 0.7 |  |
|  |  |  | Pavilion painting | -2.81 | -1.49 | -0.01 | 0.37 | -2.07 | -0.54 | -0.34 | -0.02 |  |  |  |
|  |  |  |  | 1.35 | -0.37 | -0.26 | 0.13 | -1.54 | 1.23 | -1.37 | -0.36 |  |  |  |
| Appraiser title | GIA_PCTG_StarCul |  |  |  |  |  |  |  |
| Overall cut quality | V |  |  |  |  |  |  |  |
| Symmetry appraiser title | Internal |  |  |  |  |  |  |  |
| Overall symmetry quality | VG |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  | Girdle center |  | Culet center |  | Тable center |  |  |  |
| Polish |  |  |  | Offset by table axis |  |  |  |
|  |  |  |  | Girdle-Culet | 0.75 ± 0.22, % | 0.044 ± 0.013, mm |  |  |  |
| Fluorescence |  |  |  | Girdle-Table | 0.34 ± 0.19, % | 0.020 ± 0.011, mm |  |  |  |
|  |  |  |  | Table-Culet | 0.99 ± 0.23, % | 0.058 ± 0.014, mm |  |  | Girdle to table-culet line offset | 0.21 %, 0.012 mm |