| ILLUSTRATED REPORT FOR BRILLIANT |  |  | Parameter | Avg | Min | Max | Dev | Cut | Sym |  |  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  | Diameter, mm | 5.752 | 5.745 | 5.762 | 0.29% | E | EX |  |  | 5.756 | 5.756 | 5.754 | 5.760 |  |  |  |  |
|  |  |  |  | Crown angle, ° | 34.55 | 34.41 | 34.72 | 0.31 | Grading | EX |  |  | 34.57 | 34.62 | 34.45 | 34.41 | 34.44 | 34.57 | 34.64 | 34.72 |
|  |  |  |  | Pavilion angle, ° | 40.45 | 40.21 | 40.75 | 0.54 | Grading | EX |  |  | 40.22 | 40.29 | 40.55 | 40.75 | 40.74 | 40.56 | 40.29 | 40.21 |
| Model | st4 |  |  | Total height, % | 60.35 |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |
| Expert name | Makoed A.G. |  |  | Crown height, % | 14.82 | 14.55 | 15.12 | 0.57 | E | EX |  |  | 14.55 | 14.74 | 14.67 | 14.84 | 14.80 | 15.02 | 15.12 | 14.81 |
| Report date | 11.12.2007 |  |  | Pavilion depth, % | 42.49 | 42.32 | 42.68 | 0.36 | N/A | EX |  |  | 42.44 | 42.42 | 42.49 | 42.68 | 42.65 | 42.45 | 42.32 | 42.44 |
| Real weight, ct |  |  |  | Table, % | 57.17 | 56.93 | 57.42 | 0.49 | Grading | EX |  |  | 57.42 | 57.10 | 56.93 | 57.22 |  |  |  |  |
| Calculated weight, ct | 0.70, 0.7016 |  |  | Culet, % | 0.33 | 0.30 | 0.35 | 0.05 | E | EX |  |  |  |  |  |  |  |  |  |  |
| Measurements | 5.752 (5.745-5.762) x 3.472 /0.008 mm |  |  | Girdle Bezel, % | 3.05 | 2.86 | 3.36 | 0.50 | E | EX |  |  | 3.36 | 3.18 | 3.19 | 2.86 | 2.91 | 2.88 | 2.90 | 3.10 |
| Spread | 0.01 ct, 0.72% |  |  | Girdle Bone, % | 3.01 | 2.64 | 3.35 | 0.71 |  | VG |  |  | 3.28 | 3.05 | 2.75 | 2.86 | 3.13 | 3.00 | 2.64 | 3.35 |
| AGS Spread | 0.00 ct, 0.40% |  |  | Girdle Valley, % | 1.37 | 1.10 | 1.72 | 0.62 | E | EX |  |  | 1.42 | 1.54 | 1.57 | 1.46 | 1.22 | 1.20 | 1.21 | 1.10 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | 1.41 | 1.39 | 1.46 | 1.40 | 1.13 | 1.20 | 1.52 | 1.72 |
| Average values, mm |  |  | Star: | 54.67: | 53.08: | 56.19: | 3.12 | E | VG |  |  | 55.66: | 54.26: | 54.15: | 56.19: | 55.41: | 53.98: | 53.08: | 54.67: |
|  |  |  | Upper ratio, % | 45.33 | 46.92 | 43.81 |  |  |  |  |  | 44.34 | 45.74 | 45.85 | 43.81 | 44.59 | 46.02 | 46.92 | 45.33 |
| Diam | Total height | Crown height | Pav. depth | Table | Culet | Girdle |  |  | Star angle, ° | 22.79 | 22.74 | 22.99 | 0.24 |  | EX |  |  | 22.74 | 22.74 | 22.76 | 22.99 | 22.78 | 22.77 | 22.77 | 22.75 |
|  |  |  |  |  |  | Bezel | Bone | Valley |  |  | Upper girdle angle, ° | 42.37 | 42.03 | 43.09 | 1.06 |  | VG |  |  | 42.37 | 42.40 | 42.14 | 42.12 | 43.09 | 42.81 | 42.42 | 42.27 |
| 5.752 | 3.472 | 0.852 | 2.444 | 3.289 | 0.019 | 0.175 | 0.173 | 0.079 |  |  |  |  |  |  |  |  |  |  |  | 42.47 | 42.36 | 42.05 | 42.21 | 42.03 | 42.32 | 42.38 | 42.43 |
|  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % | 79.67 | 79.06 | 80.41 | 1.35 | E | EX |  |  | 80.15 | 79.80 | 80.06 | 80.23 | 79.64 | 80.41 | 79.37 | 79.76 |
|  |  |  |  |  |  |  |  |  |  |  |  | 79.89 | 79.69 | 79.08 | 79.06 | 79.10 | 79.08 | 79.80 | 79.58 |
|  |  |  | Lower girdle angle / Halves angle, ° | 41.53 | 41.26 | 41.87 | 0.61 |  | EX |  |  | 41.33 | 41.36 | 41.38 | 41.51 | 41.71 | 41.81 | 41.85 | 41.87 |
|  |  |  |  |  |  |  |  |  |  |  |  | 41.73 | 41.73 | 41.52 | 41.45 | 41.36 | 41.31 | 41.26 | 41.30 |
|  |  |  | Twist, ° | 0.40 | 0.01 | 0.87 | 0.87 |  | EX |  |  | 0.01 | 0.09 | 0.52 | 0.87 | 0.09 | 0.51 | 0.75 | 0.36 |
|  |  |  | Crown height, mm | 0.852 | 0.837 | 0.870 | 0.033 | E | EX |  |  | 0.837 | 0.848 | 0.844 | 0.854 | 0.851 | 0.864 | 0.870 | 0.852 |
|  |  |  | Pavilion depth, mm | 2.444 | 2.435 | 2.455 | 0.021 | N/A | EX |  |  | 2.441 | 2.440 | 2.444 | 2.455 | 2.453 | 2.442 | 2.435 | 2.441 |
|  |  |  | Table, mm | 3.289 | 3.275 | 3.303 | 0.028 | Grading | EX |  |  | 3.303 | 3.285 | 3.275 | 3.291 |  |  |  |  |
|  |  |  | Culet, mm | 0.019 | 0.017 | 0.020 | 0.003 | E | EX |  |  |  |  |  |  |  |  |  |  |
|  |  |  | Girdle Bezel, mm | 0.175 | 0.164 | 0.193 | 0.029 | E | EX |  |  | 0.193 | 0.183 | 0.183 | 0.164 | 0.167 | 0.166 | 0.167 | 0.179 |
|  |  |  | Girdle Bone, mm | 0.173 | 0.152 | 0.193 | 0.041 |  | VG |  |  | 0.189 | 0.176 | 0.158 | 0.165 | 0.180 | 0.172 | 0.152 | 0.193 |
|  |  |  | Girdle Valley, mm | 0.079 | 0.063 | 0.099 | 0.035 | E | EX |  |  | 0.082 | 0.088 | 0.090 | 0.084 | 0.070 | 0.069 | 0.070 | 0.063 |
|  |  |  |  |  |  |  |  |  |  |  |  | 0.081 | 0.080 | 0.084 | 0.081 | 0.065 | 0.069 | 0.088 | 0.099 |
|  |  |  | Measurement as per OctoNus theory: |  |  |  |
|  |  |  | Crown angle, ° | 34.55 | 34.50 | 34.59 | 0.09 |  |  |  |  | 34.50 | 34.59 | 34.54 | 34.56 |  |  |  |  |
|  |  |  | Pavilion angle, ° | 40.45 | 40.42 | 40.48 | 0.06 |  |  |  |  | 40.48 | 40.43 | 40.42 | 40.48 |  |  |  |  |
|  |  |  | Fish eye effect, ° | 6.68 | N/A |  |  |  | Extra Facet / Nat | No |
|  |  |  | Culet through Crown Bezel, ° | 11.74 | N/A |  |  |  | Girdle to MIC, mm | 0.008 |
|  |  |  | Parameter, ° | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |  |  | Paint / Dug | Avg | Type | Sym | Dev | Sym |
|  |  |  | Pav. azimuths dev. from ideal | 0.00 | 0.14 | 0.42 | 0.10 | -0.44 | -0.08 | -0.61 | -0.57 |  |  | Crown, ° | 0.41 | Digging | EX | 1.36 | EX |
|  |  |  | Crown azimuths dev. from ideal | -0.01 | 0.23 | -0.09 | -0.77 | -0.35 | 0.44 | 0.14 | -0.93 |  |  | Crown, notch. | 0.1, Very small |  |  | 0.4 |  |
|  |  |  | Crown painting | 0.02 | -0.18 | -0.13 | 0.22 | 1.36 | 1.04 | 1.04 | -0.01 |  |  | Pavilion, ° | -0.09 |  | EX | -0.55 | EX |
|  |  |  |  | 0.80 | 0.45 | 0.08 | 0.50 | 0.02 | 0.59 | 0.05 | 0.77 |  |  | Pavilion, notch. | 0.0, Negligible |  |  | 0.1 |  |
|  |  |  | Pavilion painting | -0.30 | 0.02 | -0.14 | 0.20 | -0.44 | 0.18 | -0.22 | -0.29 |  |  |  |
|  |  |  |  | -0.24 | 0.07 | -0.55 | -0.03 | 0.04 | -0.20 | -0.03 | 0.43 |  |  |  |
| Appraiser title | GIA_PCTG_StarCul |  |  |  |  |  |  |  |
| Overall cut quality | V |  |  |  |  |  |  |  |
| Symmetry appraiser title | Internal |  |  |  |  |  |  |  |
| Overall symmetry quality | VG |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  | Girdle center |  | Culet center |  | Тable center |  |  |  |
| Polish |  |  |  | Offset by table axis |  |  |  |
|  |  |  |  | Girdle-Culet | 0.48 ± 0.22, % | 0.028 ± 0.013, mm |  |  |  |
| Fluorescence |  |  |  | Girdle-Table | 0.20 ± 0.20, % | 0.012 ± 0.011, mm |  |  |  |
|  |  |  |  | Table-Culet | 0.60 ± 0.24, % | 0.035 ± 0.014, mm |  |  | Girdle to table-culet line offset | 0.15 %, 0.008 mm |