| ILLUSTRATED REPORT FOR BRILLIANT |  |  | Parameter | Avg | Min | Max | Dev | Cut | Sym |  |  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant | 02.08.2008 |  |  | Diameter, mm | 5.792 | 5.784 | 5.807 | 0.40% | E | EX |  |  | 5.794 | 5.792 | 5.794 | 5.807 |  |  |  |  |
|  |  |  |  | Crown angle, ° | 39.08 | 38.84 | 39.19 | 0.34 | Grading | EX |  |  | 38.84 | 39.11 | 39.08 | 39.08 | 39.09 | 39.17 | 39.19 | 39.08 |
|  |  |  |  | Pavilion angle, ° | 40.22 | 40.15 | 40.30 | 0.14 | Grading | EX |  |  | 40.30 | 40.15 | 40.21 | 40.20 | 40.29 | 40.30 | 40.17 | 40.19 |
| Model | Simple |  |  | Total height, % | 60.89 |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |
| Expert name | Makoed A.G. |  |  | Crown height, % | 15.87 | 15.66 | 16.00 | 0.33 | E | EX |  |  | 15.66 | 15.82 | 15.77 | 15.99 | 15.89 | 16.00 | 15.96 | 15.86 |
| Real weight, ct |  |  |  | Pavilion depth, % | 42.18 | 42.05 | 42.35 | 0.31 | N/A | EX |  |  | 42.35 | 42.14 | 42.15 | 42.05 | 42.09 | 42.23 | 42.20 | 42.20 |
| Calculated weight, ct | 0.74, 0.7437 |  |  | Table, % | 61.01 | 60.91 | 61.10 | 0.19 | Grading | EX |  |  | 61.07 | 60.91 | 61.10 | 60.96 |  |  |  |  |
| Measurements | 5.792 (5.784 -5.807) x 3.527 /0.001 mm |  |  | Culet, % | 0.36 | 0.23 | 0.45 | 0.22 | E | EX |  |  |  |  |  |  |  |  |  |  |
| Spread | -0.02 ct, -2.79 % |  |  | Girdle Bezel, % | 2.85 | 2.67 | 2.97 | 0.31 | E | EX |  |  | 2.88 | 2.93 | 2.97 | 2.88 | 2.91 | 2.67 | 2.74 | 2.83 |
| AGS Spread | N/A ct, N/A % |  |  | Girdle Bone, % | 2.81 | 2.47 | 3.06 | 0.59 |  | EX |  |  | 2.93 | 2.80 | 2.66 | 3.06 | 2.89 | 2.47 | 2.86 | 2.84 |
| Extra Facet / Nat | No |  |  | Girdle Valley, % | 0.97 | 0.72 | 1.22 | 0.50 | E | EX |  |  | 1.06 | 1.05 | 1.08 | 0.96 | 1.01 | 0.87 | 0.96 | 1.22 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | 0.98 | 0.91 | 0.72 | 0.81 | 1.02 | 0.90 | 1.03 | 0.89 |
| Width | Length | Ratio (L/W) | Diameter Minimum | Diameter Maximum | Diameter Average | Total height |  |  | Star: | 61.35: | 60.76: | 62.15: | 1.39 | E | EX |  |  | 60.99: | 61.83: | 60.97: | 62.15: | 61.62: | 61.50: | 60.94: | 60.76: |
|  |  |  |  |  |  |  |  |  | Upper ratio, % | 38.65 | 39.24 | 37.85 |  |  |  |  |  | 39.01 | 38.17 | 39.03 | 37.85 | 38.38 | 38.50 | 39.06 | 39.24 |
| 5.784 mm | 5.807 mm | 1.004 | 5.784 mm | 5.807 mm | 5.792 mm | 3.527 mm |  |  | Star angle, ° | 25.74 | 25.32 | 26.00 | 0.68 |  | EX |  |  | 25.32 | 25.81 | 25.73 | 25.99 | 25.93 | 25.74 | 26.00 | 25.41 |
|  |  |  |  |  |  |  |  |  | Upper girdle angle, ° | 48.64 | 48.00 | 49.36 | 1.37 |  | VG |  |  | 48.38 | 48.51 | 48.41 | 48.99 | 48.69 | 49.00 | 48.59 | 48.79 |
|  |  |  |  |  |  |  |  |  |  |  |  | 48.40 | 48.67 | 48.90 | 49.36 | 48.30 | 48.78 | 48.00 | 48.45 |
| Crown height | Pavilion depth | Table | Culet | Girdle |  |  | Length girdle facet, % | 61.95 | 60.77 | 62.94 | 2.17 | G | EX |  |  | 61.53 | 61.91 | 62.03 | 61.69 | 61.96 | 62.48 | 61.64 | 62.45 |
|  |  |  |  | Bezel | Bone | Valley |  |  |  |  |  |  |  |  |  |  |  | 62.39 | 62.33 | 62.94 | 62.57 | 61.25 | 61.55 | 61.69 | 60.77 |
| 0.919 mm | 2.443 mm | 3.534 mm | 0.021 mm | 0.165 mm | 0.163 mm | 0.056 mm |  |  | Lower girdle angle / Halves angle, ° | 42.15 | 42.05 | 42.29 | 0.24 |  | EX |  |  | 42.15 | 42.09 | 42.19 | 42.19 | 42.18 | 42.25 | 42.13 | 42.05 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 42.15 | 42.14 | 42.21 | 42.13 | 42.06 | 42.08 | 42.19 | 42.29 |
|  |  |  | Twist, ° | 0.65 | 0.13 | 1.12 | 0.99 |  | EX |  |  | 0.31 | 1.12 | 0.93 | 0.72 | 0.42 | 0.94 | 0.13 | 0.66 |
|  |  |  |  | Crown height, mm | 0.919 | 0.907 | 0.927 | 0.019 | E | EX |  |  | 0.907 | 0.916 | 0.914 | 0.926 | 0.920 | 0.927 | 0.924 | 0.919 |
|  |  |  |  | Pavilion depth, mm | 2.443 | 2.436 | 2.453 | 0.018 | N/A | EX |  |  | 2.453 | 2.441 | 2.441 | 2.436 | 2.438 | 2.446 | 2.444 | 2.444 |
|  |  |  |  | Table, mm | 3.534 | 3.528 | 3.539 | 0.011 | Grading | EX |  |  | 3.537 | 3.528 | 3.539 | 3.531 |  |  |  |  |
|  |  |  |  | Culet, mm | 0.021 | 0.013 | 0.026 | 0.013 | E | EX |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  | Girdle Bezel, mm | 0.165 | 0.155 | 0.172 | 0.018 | E | EX |  |  | 0.167 | 0.170 | 0.172 | 0.167 | 0.168 | 0.155 | 0.159 | 0.164 |
|  |  |  |  | Girdle Bone, mm | 0.163 | 0.143 | 0.177 | 0.034 |  | EX |  |  | 0.170 | 0.162 | 0.154 | 0.177 | 0.168 | 0.143 | 0.165 | 0.164 |
|  |  |  |  | Girdle Valley, mm | 0.056 | 0.042 | 0.071 | 0.029 | E | EX |  |  | 0.061 | 0.061 | 0.063 | 0.055 | 0.059 | 0.051 | 0.056 | 0.071 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | 0.057 | 0.053 | 0.042 | 0.047 | 0.059 | 0.052 | 0.060 | 0.052 |
|  |  |  |  | Measurement as per OctoNus theory: |  |  |  |
|  |  |  |  | Crown angle, ° | 39.08 | 38.96 | 39.14 | 0.18 |  |  |  |  | 38.96 | 39.14 | 39.13 | 39.08 |  |  |  |  |
|  |  |  |  | Pavilion angle, ° | 40.22 | 40.19 | 40.29 | 0.10 |  |  |  |  | 40.29 | 40.23 | 40.19 | 40.20 |  |  |  |  |
|  |  |  |  | Fish eye effect, ° | 3.44 | N/A |  |  |  | MIC, mm | 5.784 |
|  |  |  |  | Culet through Crown Bezel, ° | 7.53 | N/A |  |  |  | Girdle to MIC, mm | 0.001 |
|  |  |  |  | Parameter, ° | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |  |  | Paint / Dug | Avg | Type | Sym | Dev | Sym |
|  |  |  |  | Pav. azimuths dev. from ideal | 0.00 | -0.27 | -0.21 | -0.04 | 0.24 | -0.30 | 0.35 | -0.22 |  |  | Crown, ° | -0.14 |  | EX | -0.83 | EX |
|  |  |  |  | Crown azimuths dev. from ideal | 0.31 | 0.85 | 0.73 | 0.68 | 0.66 | 0.64 | 0.47 | 0.44 |  |  | Crown, notch. | 0.0, Negligible |  |  | 0.2 |  |
|  |  |  |  | Crown painting | 0.11 | -0.12 | -0.59 | 0.15 | -0.07 | 0.46 | -0.69 | 0.43 |  |  | Pavilion, ° | 0.25 |  | EX | 1.36 | EX |
|  |  |  |  |  | -0.83 | 0.01 | -0.38 | 0.69 | -0.68 | 0.20 | -0.83 | -0.07 |  |  | Pavilion, notch. | 0.1, Negligible |  |  | 0.4 |  |
|  |  |  |  | Pavilion painting | 0.23 | -0.25 | 1.36 | -0.02 | 0.99 | 0.64 | 0.20 | 0.16 |  |  |  |
|  |  |  |  |  | -0.33 | -0.38 | 0.48 | 0.41 | -0.05 | -0.15 | 0.78 | -0.13 |  |  |  |
| Appraiser title | GIA_PCTG_StarCul |  |  |  |  |  |  |  |
| Overall cut quality | G |  |  |  |  |  |  |  |
| Symmetry appraiser title | Internal |  |  |  |  |  |  |  |
| Overall symmetry quality | VG |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  | Girdle center |  | Culet center |  | Тable center |  |  |  |
| Polish |  |  |  | Girdle-Culet offset by table axis | 0.13 ± 0.22, % | 0.008 ± 0.013, mm |  |  |  |
|  |  |  |  | Girdle-Table offset by table axis | 0.07 ± 0.20, % | 0.004 ± 0.011, mm |  |  |  |
| Fluorescence |  |  |  | Table-Culet offset by table axis | 0.18 ± 0.24, % | 0.011 ± 0.014, mm |  |  |  |
|  |  |  |  | Girdle to table-culet line offset | 0.04 %, 0.002 mm |  |  |  |